1. General

# A. Name and Description

Sentry Steel Shingle

Sentry Steel Shake
Sentry Steel Slate

The steel panels are designed to simulate the look of asphalt, wood, and slate shingles. The panels are for use on residential and light commercial roofs, sidewalls, and mansards

Exposure Height: 12.0”

Exposure Width: 39.0”

Weight /Square: 76.0 lb.

# B. Provider

Sentry Metal Roofing / Best Buy Metals

1652 S Lee Hwy
Cleveland, TN 37311

Tel: 800.728.4010

Fax: 423.728.3606

Email: info@bestbuymetals.com

Web address:

www.bestbuymetals.com

# C. Scope

The scope of the work includes, but is not limited to, the installation of all pre-formed panels, pre-formed accessories and field-formed accessories such as miscellaneous flashings and attaching devices.

2. Product

# A. Material

All steel materials, including pre-formed panels, pre-formed accessories and flashings and matching coilstock are made of galvanized, ASTM A653, G90, CS type B .0142” (29 gauge) steel sheet stock.

# B. Finish

Sentry Steel Shingles/Shake/Slate are coated with a Kynar 500 or Hylar 5000 base coat and protective primer to provide a high quality finish.

# C. Additional Materials

Other materials available from the manufacturer include touch-up paint, underlayment, and nails.

3. Installation

# A. Pitch

Sentry Steel Shingles/Shakes are designed to be installed on roofs with a 3:12 or greater pitch.

# B. Decking

The panels are applied over minimum ½” decking. The system may also be applied over existing composition roofing (single or multi-layered).

# C. Underlayment

In the case of either a new roofing application or re-roofing, the entire roof must be covered with at least one layer of 30 lb. felt underlayment or equivalent.

# D. Panels

Sentry Steel Shingles/Shake/Slate panels have a four-way interlock that locks each panel to the surrounding panels. Successive courses are staggered to provide a random appearance. The panels are secured to the deck with an integrated nailing flange at the top of each shingle panel. Each full panel requires four fasteners.

# E. Fasteners

On installations over plywood or similar decking, hot-dipped galvanized steel ring shank roofing nails, zinc plated/galvanized steel screws, or stainless steel screws of sufficient length to fully penetrate the decking.

4. Protective Properties

# A. Wind Resistance

Sentry Steel Shingles/Shake/Slate has passed the U.L. 580 Class 90 uplift test.

# B. Fire Resistance

Fire-Test-Response Characteristics as determined per test method ASTM 108: Class A fire rating

# C. Impact Resistance

The Sentry Steel Shingles/Shake/Slate meet UL 2218 Class 4 impact resistance.

D. Appraisal Certificates

Texas Department of Insurance product evaluation RC-112.